## Slide 1: Electric transport in different granitic rocks
H.G. Silva1,*, M.P.F. Graça2, J. H. Monteiro2, M. Bezzeghoud1, R.N. Rosa1, S. K. Mendiratta2, M. Tlemçani1, P. Moita1
1Geophysics Center of Évora and Physics Department, University of Évora, Portugal 2Physics Department, University of Aveiro, I3N, University of Aveiro, 3810-193 Aveiro, Portugal
*hgsilva@uevora.pt

## Slide 2: Outline
Project
Samples
Samples preparation
Measurements:
4.1. Impedance spectroscopy (ε-f)
4.2. I-V characteristics
Conclusions and future work

## Slide 3: Our project
Atmospheric electric field sensor.
Radio receiver for very low and low frequencies.
Meter of atmospheric Radon levels
(in installation).
Magnetometers for ultra-low frequencies (planned).

## Slide 4: Our project

## Slide 5: Samples
YC is a porphiritic coarse grained biotitic-muscovitic granite, yellow coloured and characterized by an abundance of large feldspar usually showing poorly defined shapes.
YC
GM
RM
GM is a granodiorite grey coloured and medium grained rock with homogeneous appearance. Dark minerals is mainly biotite.
RM is a granite with a homogeneous medium grained matrix (occasionally coarser grained quartz) and light rosy coloured determined by the tonality of the feldspar crystals that stand out from a greyish matrix.

## Slide 6: Samples
YC
RM
GM
biotite
muscovite
plagioclase
quartz
Alkaline feldspar
biotite
quartz
plagioclase
Alkaline feldspar
biotite
Alkaline feldspar
plagioclase
quartz
Samples
microphotographs

## Slide 7: Samples preparation
Circular samples with approximately 24 mm diameter and 2-4 mm in thicknesses were prepared. Once cut and carefully polished (with a 15µm polishing disc) the samples here heated from room-temperature (RT) up to ~400 K and after cooled down again.
Circular electrodes with a diameter of 20 mm were then established using silver conductive paint (in the future, new contacts will be tested). The samples were submitted again to a heat treatment at ~400 K to evaporate the silver paint solvent.

## Slide 8: Measurements
Current-Voltage characteristics (I-V): were done at stabilized temperatures ranging from 100 K to 300 K using a Keitheley 6487 Picoammeter/Voltage Source.
Impedance spectroscopy (ε-f): were done with VAC = 1 V test signal in the frequency range of 40 Hz to 1 MHz at stabilized temperatures ranging from 100 K to 360 K. It was used an Agilent 4294A Precision Impedance Analyzer.
C
R
N2
He
vacuum
sample

## Slide 9: Impedance spectroscopy
YC
Impedance spectra at different temperatures: a) Real part of the dielectric constant; b) Imaginary part of the dielectric constant.
Real and Imaginary part of e as a function of temperature: a) f = 100 Hz; b) f = 1027 Hz; c) f = 10 520 Hz; d) comparison.

## Slide 10: Impedance spectroscopy
GM
Impedance spectra at different temperatures: a) Real part of the dielectric constant; b) Imaginary part of the dielectric constant.
Real and Imaginary part of e as a function of temperature: a) f = 100 Hz; b) f = 1027 Hz; c) f = 10 520 Hz; d) comparison.

## Slide 11: Impedance spectroscopy
RM
Impedance spectra at different temperatures: a) Real part of the dielectric constant; b) Imaginary part of the dielectric constant.
Real and Imaginary part of e as a function of temperature: a) f = 100 Hz; b) f = 1027 Hz; c) f = 10 520 Hz; d) comparison.

## Slide 12: I-V characteristics
GM
I-V characteristics for GM at different temperatures. The inset shows a detail of the I-V curves in the temperature range from 180 K up to 280 K.
Current as a function of the temperature for different voltage levels: a) V = 5 V; b) V = 10 V; c) V = 50 V; d) Arrhenius plot with a linear fit (shown by cyan line).
Ea ~ 26 meV

## Slide 13: Conclusions and future work
An anomaly in the dielectric behavior near T~220 K is found.
This temperature is typical of the super-cooled phase transition of strongly confined water affecting electronic devises.
Samples YC and RM show a relaxation process taking place at f~103 Hz readily evidenced in the K’’ curves here a significant peak appears at this frequency that does not change with temperature.
The I-V curves of GM sample are strongly thermal activated with typical energy of Ea~26 meV.
Our final objective is to Investigate possible mechanisms of charge creation in different crust materials and conditions (pressure and temperature).

## Slide 14: Acknowledgments
Support
Team
Collaborations

## Slide 15: Thank you for attention
Almendres Cromlech at Évora
http://en.wikipedia.org/wiki/Almendres_Cromlech