## Slide 1: Why is Snow Slippery? The Role of Abrasion in Snow Kinetic Friction
James H. Lever, Susan Taylor, Garrett R. Hoch, Emily Asenath-Smith
Engineer Research and Development Center (ERDC - CRREL)
Lever et al. (2018) The mechanics of snow friction as revealed by micro-scale interface observations.
J. Glaciology, 64(243) 27 – 36.
Lever et al. (2019) Evidence that abrasion can govern snow kinetic friction. J. Glaciology, 65(249) 68–84.
US Army ERDC 6.1 basic research, military engineering

## Slide 2: Why is snow slippery?
Reynolds (1899) – water lubrication from pressure melting
Bowden & Hughes (1939) – water lubrication from frictional heating
Issues to implement theory
Mixed friction modes along a slider
m is average value – must separately measure & scale each mode
Persistent contacts are required
Snow is weak – easy to deform or fail grains
Many studies used ice as a surrogate
No micro-scale observations of self-lubrication
Unknown evolution of contact area
How does transition occur from dry to lubricated contact?
What is fate of melt-water (squeezing, shearing, plowing by asperities)?
Predicted water layers are thinner than slider roughness
How does water layer support slider?

## Slide 3
Original Objectives
Confirm self-lubrication
Map dry-to-lubricated transition
Quantify evolution of real contact area
Quantify production & loss of melt water
Approach
Ring tribometer – single friction mode
High-res IR camera to measure temperature & area evolution
Optical, SEM and micro-CT to track melt water and changes in snow structure
Tribometer
Polyethylene ring rotated on stationary snow
Snow Samples
Compacted & sintered “strong” snow
Test parameters
0.3 – 1.3 m/s, 0.8 – 4.5 kPa, -4 – -19°C
IR Camera
15-mm pixels, Ac/An = 3 x 10-6
10 x 8 mm snow patch imaged each slider revolution
Accuracy ± 0.1°C near 0°C

## Slide 4: Key Result: No Melting
Mode 1 – Cascading grain-bond failure at low friction
m < 0.03
No persistent contacts to melt
Snow warmed very little, Tmax < 0°C
Mode 2 – Dry-contact abrasion at low friction
m < 0.05
Slider abraded persistent contacts
Grains warmed but didn’t melt, Tmax < 0°C
Polished flat-top grains yielded glazed macro-surface
IR movies: evolving snow-grain contacts are closed contours

## Slide 5: Coordinated IR, Optical and SEM Images Reveal Structure
IR
Optical
SEM
Abrasion polishes snow-grain contacts
Abraded wear particles deposit & sinter in pore spaces – ”lacy” structures
Sintered deposits can fill pores & flatten with further sliding
Infilled pores
Post-test
debris
Undisturbed
snow
Abraded grains
& infilled pores

## Slide 6: Towards a New Theory: Dry-Contact Abrasion
Abrasive wear – Archard (1953) W ∝ P/H
W is volumetric wear rate, P is load
H(T) is indentation hardness of snow grains (ice), H(0°C) → 0
Abrasion accelerates as T → 0°C
Sliding Heat Source – Tian & Kennedy (1993, 1994)
Tcontact = Tflash + Tnominal + Tbackground
Match temperature across contact to determine heat-flux split
Qslider + Qgrain = Qfriction
Uniform temperatures measured across contacting grains, Ac/An ~ 0.01 – 0.3
Predicts Tflash << Tnominal
Most of heat initially flows into slider

## Slide 7: Model Predictions: Contact Area & Temperature
Tribometer Tests
Use measured m
Good agreement with measured area (black) and temperature (red) evolution
Model predicts no melting
Field Data – Sleds
Use measured m
Predict steady-state temperature profiles along sled-snow interface
Tnominal ≈ Tcontact for small Tflash
Data confirm contact temperatures < 0°C
Antarctica
Greenland

## Slide 8: Why is Snow Slippery?
  Intergranular bonds may initially break
  Abrasion gets easier as contacting grains warm up
  Layer of abraded particles might act as dry lubricant
  Apply dry-lubricant theory to snow friction
    Need to measure rheological properties of wear particles
    One mechanism postulates fluid-like behavior
  Observe single snow-grain/slider contact at high-res
    Continuous IR and microscope video of evolving contact
  Does self-lubrication occur on ice?
    Abraded particles trapped under skate could melt
On-Going Work
Thanks!