## Slide 1
Nimrod Carmon and Eyal Ben-Dor*
Porter School of Environmental and Erath Science
Faculty of Exact Science
Tel Aviv University, Tel Aviv, Israel
*Correspondence: bendor@post.tau.ac.il
Mapping the Friction Coefficient of Asphalt Roads Using Airborne Imaging Spectroscopy

## Slide 2
Outline
Friction coefficient and asphalt roads – Tradition Measurements
Spectral ground measurements: Proof of concept for optical HSR sensors
Optical HSR Airborne measurements: Road mapping
Spectral ground measurements: Proof of concept for thermal hsr sensors
Thermal HSR Airborne measurements: Road mapping
Future Ideas

## Slide 3: Asphalt Composition
“composite material composed of mineral aggregate adhered with a binder”
Micro and Macro textures which creates high friction with the rubber tire
The binder material, usually Bitumen, binds the aggregates together
Aging effects may degrade the binder, exposing the minerals and reducing the asphalt’s firmness and reducing friction with tires

## Slide 4: Friction Coefficient of Roads
Dynamic\Kinetic Friction Coefficient
Ff = μ N
where
Ff = frictional force (N, lb)
μ = static (μs) or kinetic (μk) frictional coefficient
N = normal force (N, lb)

## Slide 5: Dynamic Friction Mapping Today
The 5th wheel concept
Mechanical system
Many disadvantages

## Slide 7: VIS-NIR-SWIR region Ground
Spectrometer acquisition
  Sensor: ASD
  Research Area: 5km segment of Road 4
  Flight height: 40 cm
  Spectral sensitivity: VIS-NIR-SWIR
  Spectral resolution: 2150 bands

## Slide 8
Wavelength (nm)
Reflectance

## Slide 9: Data Processing
Processing Steps:
Pairing
Merging
Modeling
~30m
~10m

## Slide 10: Machine Learning
Spectral Information Chemical Attribute
We need a BIG dataset of samples for creating a VALID correlation model
Then, we can predict the chemistry from the spectral data
pH
COx
Salt
Clay
Minerals

## Slide 11
PARACUDA II
Machine Learning Analysis

## Slide 12: Modeling

## Slide 13: Airborne –VNIR-SWIR
Aerial acquisition campaign
380-2500nm
4.5-14nm

## Slide 14
Working Scheme
Data Acquisition over a selected high way “latron”
Acquisition with the FENIX1K sensor
Friction Coefficient by the “Israel ways”
Geo rectification – FENIX 1K
Data Mining Full spectrum (PLS + field Model)
Atmosphere Correction

## Slide 16: Calibration (b) validation ( c )

## Slide 17
Wavelength (nm)
B Coefficient
VNIR
SWIR-1
SWIR-2

## Slide 18
Measured (Mu)
Predicted (Mu)
R2 = 0.6316
RMSEP = 0.0776
RPD = 1.6462
N= 1332
P<0.0001
R2 = 0.702
RMSEP = 0.0696
RPD = 1.8325
N= 333
P<0.0001
Measured (Mu)
Predicted (Mu)
(a)
(b)

## Slide 21: TIR region Ground
Chart: Wavelength (Microns)
| 7.6123775871068684 | 7.688522484832208 | 7.7662061004861407 | 7.8454139324925123 | 7.9263169889757492 | 8.0089059995784027 | 8.0931686546705919 | 8.1792901981866226 | 8.2671959312274321 | 8.3570816103600851 | 8.448943351318464 | 8.5427739888619794 | 8.6387868262778813 | 8.7369814465979019 | 8.8373568158965927 | 8.9401453327369182 | 9.0453530828655957 | 9.1529826304150674 | 9.2632902572087694 | 9.3762010708467347 | 9.4919885812896094 | 9.6106715974793939 | 9.7322652846953783 | 9.8570724494825033 | 9.9851222676723896 | 10.116470929814961 | 10.251363641517276 | 10.389891062397416 | 10.532213629548499 | 10.67850130510347 | 10.828897797844766 | 10.983603700559733 | 11.142781160869138
F | 12.1962 | 13.7967 | 13.735 | 13.5203 | 13.6092 | 14.5389 | 14.4528 | 14.4728 | 14.4865 | 14.6933 | 14.6901 | 14.7393 | 14.9041 | 14.8118 | 14.7969 | 14.8157 | 14.8487 | 14.82 | 14.7892 | 14.7732 | 14.881 | 14.7291 | 14.7226 | 14.5852 | 14.4628 | 14.3311 | 14.2456 | 14.0822 | 13.9536 | 13.8006 | 13.6172 | 13.4182 | 12.7394
G | 12.3462 | 14.0406 | 13.9341 | 13.7326 | 13.8075 | 14.7984 | 14.6702 | 14.7251 | 14.7042 | 14.9544 | 14.891 | 14.9992 | 15.1136 | 15.0605 | 14.9872 | 15.0593 | 15.0288 | 15.0441 | 14.9617 | 15.0038 | 15.0641 | 14.9376 | 14.8926 | 14.7795 | 14.6113 | 14.4975 | 14.3949 | 14.243 | 14.097 | 13.955 | 13.762 | 13.5644 | 12.8658
A | 15.4398 | 18.2544 | 17.8804 | 17.3282 | 17.5246 | 19.1439 | 18.7061 | 18.7756 | 18.6476 | 18.8257 | 18.7259 | 19.1285 | 19.3238 | 18.9345 | 18.4909 | 18.3673 | 18.5332 | 18.321 | 18.1777 | 18.1988 | 18.5469 | 18.4166 | 18.3874 | 18.1248 | 17.9238 | 17.5703 | 17.5873 | 17.1408 | 16.5936 | 16.3581 | 15.8576 | 15.8662 | 15.7673
B | 8.4852 | 8.9482 | 8.6834 | 9.1746 | 8.7234 | 8.4027 | 6.4124 | 7.619 | 6.5455 | 5.4074 | 6.2666 | 5.8278 | 4.7631 | 5.3867 | 4.7321 | 4.6304 | 5.1755 | 4.6649 | 4.6963 | 6.3405 | 7.5533 | 6.5389 | 7.1087 | 6.4276 | 5.149 | 4.4675 | 5.4221 | 4.9769 | 5.4518 | 5.1066 | 5.485 | 5.6292 | 5.2433
C | 11.5213 | 12.8668 | 12.5802 | 12.5406 | 12.207 | 12.5898 | 11.4954 | 11.3468 | 10.7855 | 10.672 | 10.789 | 11.1383 | 11.5382 | 10.9351 | 10.5696 | 10.4435 | 10.6436 | 10.514 | 10.6874 | 11.7815 | 12.9228 | 12.9579 | 13.1791 | 13.1405 | 13.1023 | 13.0726 | 13.1302 | 13.0549 | 13.0158 | 12.9057 | 12.8049 | 12.6803 | 12.5174
D | 11.5141 | 12.7511 | 12.7088 | 12.6329 | 12.6883 | 13.4458 | 13.3783 | 13.4042 | 13.4232 | 13.6808 | 13.6172 | 13.7279 | 13.8642 | 13.8071 | 13.8075 | 13.8936 | 13.8384 | 13.8568 | 13.7998 | 13.7473 | 13.7414 | 13.6617 | 13.6777 | 13.6103 | 13.5469 | 13.4964 | 13.4434 | 13.3655 | 13.2814 | 13.1768 | 13.0716 | 12.8741 | 12.6586
E | 9.505 | 10.0637 | 10.1855 | 10.2033 | 10.3092 | 10.6026 | 10.6937 | 10.7647 | 10.8529 | 10.9755 | 11.0143 | 11.0847 | 11.1697 | 11.2119 | 11.2614 | 11.3097 | 11.3206 | 11.3461 | 11.361 | 11.358 | 11.3628 | 11.3343 | 11.3301 | 11.2929 | 11.254 | 11.2041 | 11.1414 | 11.0793 | 11.0121 | 10.9393 | 10.8645 | 10.7567 | 10.6159

## Slide 22: Airborne –LWIR
Aerial acquisition campaign
7.6-11.7 mm
4cm-1; 70 bands
www.telops.com
www.telops.com

## Slide 23: Airborne Operation
Collect airborne data of roads (RAD)
Obtain DFC data (Vehicle)
Correct spectral cubes for atmospheric attenuation and TES (FLASH IR)
Develop geometric tools for developing a dataset (TAU tool box)
Analyze dataset with data mining methods

## Slide 24
Radiance
Plank Fit
Atmosphere Correction
Emissivity Separation
TAU tool box
FLASH IR
Geometric Correction
TELOPS

## Slide 27
a |  |  |  | 
Min | Max | Mean | Std | n
0.22 | 0.634 | 0.45 | 0.073 | 1055

## Slide 28
EMISIVITY AND FRICITION COEF

## Slide 31
All Bands
88

## Slide 33
11.5
11.1
10.3
9.4

## Slide 34
4 Selected Bands
9.4, 10.3, 11.1 11.5

## Slide 35
Road Margin
Road Asphalt

## Slide 36
HSR-TIR sensor
Forward Looking TIR sensor
The Vision

## Slide 37: Conclusions
Airborne Hyperspectral Remote Sensing is capable to map the friction coefficient (FC) in asphaltic roads in both optical and thermal spectral regions
The VIS-NIR-SWIR is limited to day acquisition
The TIR is available is open for day and night acquisition
The FC can be extracted using only 4 channels only from the LWIR region .
Future vision: adopting the technology for safty driving and autonomous cars

## Slide 38
Thank you for your attention!