## Slide 1
Do chemical characteristics affect the potential of biochars to adsorb cations?
Heike Knicker1*
Jose Maria Garcia Castro de Barragan1.2.
Elena Fernandez-Boy2. Michael Knicker3. Regina León Ovelar1.2.4
1 Instituto de Recursos Naturales e Agrobiologia de Sevilla (IRNAS-CSIC). Sevilla. Spain
2 Departamento de Cristalografía. Mineralogía y Química Agrícola. Universidad de Sevilla. Sevilla. Spain
3 Consult Michael Knicker (CMK). München. Germany
4 Laboratorio de Química*. Facultad de Ingeniería. Universidad Nacional de Asunción. San Lorenzo. Paraguay
*knicker@irnase.csic.es
© Authors, all rights reserved

## Slide 2
Cu
Summary: Reasoning
Revealing relationship between chemical composition and adsorption efficiency
Using pyrochars with different aromaticity and chemical composition may contribute to a better understanding of the adsorption mechanism
NMR Relaxometry on Cu2+- doted pyrochars allows the determination of C-groups involved in the adsorption of cations
Biochar adsorbs cations:
  use as filter for heavy metals
  soil amendment with nutrients storage capacity
As a paramagnetic Ion, Cu2+ shortens the Spin-Lattice Relaxation time (T1) of the 13C and its 1H to which it is adsorbed.
© Authors, all rights reserved

## Slide 3
Cu
Summary: Results
The Adsorption to the three pyrochars used in this study was best fitted with the Freundlich model
The adsorption efficiency increased with aromaticity of the sample
We found indications that crystalline domains of weakly charred pyrochars from cellulosic feedstock did not allow Cu2+ to access all potential adsorption sites
Aside from charged functional groups, π-orbitals of aromatic rings contributed to Cu2+ adsorption
Porosity is not the main factor determining Cu2+ adsorption to pyrochar;
Accessibility of Cu2+ to pores and the availability of π-orbitals of aromatic rings seem also to play an important role.
© Authors, all rights reserved

## Slide 4
Introduction: Organic Waste - a Valuable Resource
Industry
Agriculture
ORGANIC
WASTE
Valorization:
Biochar
Definition:
Ecologically sustainable organic feedstock
Heterogeneous substance
High aromaticity
High organic C content
EBC (2012)
Pyrolysis (low oxygen)
Soil amendment
Slow-release fertilizer
Gardening soil
Water clean-up
Soil remediation
Filter (water clean-up)
etc.
Material with:
High porosity
High waterholding capacity
Cation adsorption
© Authors, all rights reserved

## Slide 5
But: Biochar ≠ Biochar!
Biochar structure depends on:
Feedstock
Production conditions
400ºC. 3h
500ºC. 3h
450ºC. 0.5h
Chitin(Ch0)
Peat (Pe0)
Acrocomia endocarp
(Ac0)
Chitin char (Ch400)
Peat char (Pe500)
Acrocomia endocarp char
(Ac450)
© Authors, all rights reserved

## Slide 6
Material | C g kg-1 |  | H g kg-1 |  | N g kg-1 |  | Ash g kg-1 |  | O* g kg-1 | H/Catm | C/N (w/w) | O/Catm | pH (H2O) |  | SBET m2g-1
Ch0 | 437.7 | ± 2.0 | 64.4 | ± 0.7 | 63.8 | ± 0.4 |  |  |  | 1.8 | 6.9 |  | 6.9 | ± 0.0 | 
Ch400 | 700.1 | ± 2.2 | 28.0 | ± 0.1 | 86.1 | ± 1.0 | 11.8 | ± 0.1 | 143.7 | 0.5 | 8.1 | 0.2 | 6.4 | ± 0.0 | 216
Pe0 | 429.0 | ± 8.8 | 49.5 | ± 2.0 | 8.7 | ± 0.3 |  |  |  | 1.4 | 49.2 |  | 6.2 | ± 0.1 | 
Pe500 | 684.1 | ± 3.7 | 26.8 | ± 0.5 | 14.3 | ± 0.3 | 140.1 | ± 1.3 | 134.8 | 0.5 | 47.9 | 0.1 | 8.4 | ± 0.1 | 192
Ac0 | 487.4 | ± 1.7 | 55.8 | ± 0.4 | 1.8 | ± 0.0 |  |  |  | 1.4 | 264.4 |  | 5.9 | ± 1.2 | 
Ac450 | 564.8 | ± 2.5 | 46.7 | ± 0.2 | 2.8 | ± 0.1 | 16.8 | ± 0.1 | 368.8 | 1.0 | 202.7 | 0.5 | 7.3 | ± 0.1 | 178
Table 1: Elemental composition of chitin, peat and Acrocomia endocarp and their chars produced at 400°C, 500°C and 450°C, respectively. the pH (H2O) and the BET surface area (SA) (CO2) of the chars.
*Calculated by the sum of ash. C. H. and N contents subtracted from 1000 g of sample material.
© Authors, all rights reserved

## Slide 7
Carboxyl
Aromatic
O/N-
Alkyl
Alkyl
Carboxyl
Aromatic
O/N-
Alkyl
Alkyl
200
100
0
300
-100 ppm
200
100
0
300
-100 ppm
Ch0
Ch400
Ac0
Pe0
Ac450
Pe500
103
83
75
60
55
23
73
172
172
155
129
116
105
73
62
33
172
157
132
116
104
72
64
56
20
158
127
72
32
20
155
127
72
39
18
169
172
154
131
116
104
72
64
56
20
33
Chemical Composition Determined by Solid-state 13C NMR Spectroscopy
Bruker Avance III 400 MHz
Cross-polarization: 1 ms
Magic angle spinning: 14 kHz
Difference in aromaticity (160-90 ppm):
Pe500 > Ch400 > Ac450
Difference in polarity P:
I(225-140 ppm) + I(90 – 45 ppm)
P =
I(140-90 ppm) + I(45-0 ppm)
Ac450 > Ch400 > Pe500
© Authors, all rights reserved

## Slide 8
Different chemical compostion, polarity, pH and BET surface (CO2) may lead to:
Differences in the Cation Adsorption?
Differences in the Adsorption Mechanism?
Adsorption experiments with paramagnetic Cu2+
NMR-Relaxometry:
Relaxation time is affected by paramagnetic Cu2+
Determination of affected C group allows identification of binding site
Hypothesis:
© Authors, all rights reserved

## Slide 9
Cu
Langmuir
Freundlich
copyright: freepng.es
Adsorption of Cu2+ onto Biochar: Experimental Design
200 mg biochar + Cu(NO3)2 (0.9-17 mM)
Shaking for 24 h at 25ºC
Separation of solid and liquid phase
Determination of Cu2+ concentration in the solution (Ce)
Calculation of Cu2+ concentration in solid (Qe)
Qmax: maximum adsorption capacity (mmol g−1)
K: Langmuir constant (L mg−1)
Kd: Freundlich distribution coefficient.
n: correction factor constant
© Authors, all rights reserved

## Slide 10
Chart: Adsorptión Isotherme (Qe vs Ce)
| 0.24 | 1.08 | 2.84 | 4.55 | 6.15 | 8.5 | 11.4 | 12.6 | 13.8 | 14.6 | 0.1 | 1.1100000000000001 | 2.9 | 4.8 | 6.4249999999999998 | 11.1 | 13.100000000000001 | 11.4 | 15 | 0.29000000000000004 | 1.1000000000000001 | 3.13 | 4.6749999999999998 | 6.4750000000000005 | 7.3999999999999995 | 9 | 11.1
Qe vs ce | 0.07625 | 0.093125 | 0.15125 | 0.1875 | 0.23125 | 0.2875 | 0.2 | 0.2625 | 0.275 | 0.3 | 0.09375 | 0.089375 | 0.14375 | 0.15625 | 0.19688 | 0.2375 | 0.2 | 0.2 | 0.25 | 0.07 | 0.090625 | 0.115 | 0.17188 | 0.19062 | 0.1625 | 0.225 | 0.2375
Chart: ln Qe vs Ce
| 0.24 | 1.08 | 2.84 | 4.55 | 6.15 | 8.5 | 11.4 | 12.6 | 13.8 | 14.6 | 0.1 | 1.1100000000000001 | 2.9 | 4.8 | 6.4249999999999998 | 8.5 | 11.1 | 13.100000000000001 | 11.4 | 15 | 0.29000000000000004 | 1.1000000000000001 | 3.13 | 4.6749999999999998 | 6.4750000000000005 | 7.3999999999999995 | 9 | 11.1 | 13.4
Ln Qe | -2.5737 | -2.3738 | -1.8888 | -1.674 | -1.4643 | -1.2465 | -1.6094 | -1.3375 | -1.291 | -1.204 | -2.3671 | -2.4149 | -1.9397 | -1.8563 | -1.6252 | -1.2465 | -1.4376 | -1.6094 | -1.6094 | -1.3863 | -2.6593 | -2.401 | -2.1628 | -1.761 | -1.6574 | -1.8171 | -1.4917 | -1.4376 | -1.1239
Chart: Freundlich
| -1.4271163556401458 | 7.6961041136128394E-2 | 1.0438040521731147 | 1.5151272329628591 | 1.8164520818184267 | 2.1400661634962708 | 2.4336133554004498 | 2.5336968139574321 | 2.6246685921631592 | 2.6810215287142909 | 0.10436001532424286 | 1.0647107369924282 | 1.5686159179138452 | 1.8601966307812834 | 2.1400661634962708 | 2.4069451083182885 | 2.5726122302071062 | 2.4336133554004498 | 2.7080502011022101 | -1.2378743560016172 | 9.5310179804324935E-2 | 1.1410330045520618 | 1.5422291627406504 | 1.8679486075856016 | 2.0014800002101238 | 2.1972245773362196 | 2.4069451083182885 | 2.4849066497880004 | 2.5952547069568657
Ln Qe | -2.5737 | -2.3738 | -1.8888 | -1.674 | -1.4643 | -1.2465 | -1.6094 | -1.3375 | -1.291 | -1.204 | -2.4149 | -1.9397 | -1.8563 | -1.6252 | -1.2465 | -1.4376 | -1.6094 | -1.6094 | -1.3863 | -2.6593 | -2.401 | -2.1628 | -1.761 | -1.6574 | -1.8171 | -1.4917 | -1.4376 | -1.0862 | -1.1239
Chart: Langmuir
| 0.24 | 1.08 | 2.84 | 4.55 | 6.15 | 8.5 | 11.4 | 12.6 | 13.8 | 14.6 | 1.1100000000000001 | 2.9 | 4.8 | 6.4249999999999998 | 8.5 | 11.1 | 13.100000000000001 | 11.4 | 15 | 0.29000000000000004 | 1.1000000000000001 | 3.13 | 4.6749999999999998 | 6.4750000000000005 | 7.3999999999999995 | 9 | 11.1 | 12 | 13.4
Ce/Qe | 3.1475 | 11.5973 | 18.7769 | 24.2667 | 26.5946 | 29.5652 | 57 | 48 | 50.1818 | 48.6667 | 12.4196 | 20.1739 | 30.72 | 32.6349 | 29.5652 | 46.7368 | 65.5 | 57 | 60 | 4.1429 | 12.1379 | 27.2174 | 27.2 | 33.9672 | 45.5385 | 40 | 46.7368 | 35.5556 | 41.2308
Adsorption Isotherms of Cu2+ to Ch400
© Authors, all rights reserved

## Slide 11
 | Freundlich |  |  | Langmuir |  | 
 | R2 | Kd | n | R2 | Qmax (mg/g) | K (l/mg)
Ch400 | 0.8596 | 0.1122 | 2.7480 | 0.8392 | 19.63 | 2.142
Pe500 | 0.8854 | 0.1177 | 2.4624 | 0.848 | 25.73 | 1.973
Ac450 | 0.568 | 0.0144 | 1.0618 | 0.3426 | 12.84 | 1.227
Adsorption Parameters of Cu2+ to Ch400, Pe500,
Ac450
Better R2 with Freundlich: non-ideal adsorption on a heterogeneous surface
n > 1: higher Cu2+-concentration decreases relative adsorption
Kd (Adsorption affinity): Pe500> Ch400 > Ac450 (very low adsorption)

## Slide 12
Biochar | Single point surface area at P/Po (m²/g) | BET Surface Area (CO2) | pH | Aromaticity | Polarity
Quitina (Ch) | 163.36 | 216.13 | 6.4 | 74 | 0.32
Turba (Pe) | 158.89 | 192.41 | 8.4 | 88 | 0.27
Acrocomia (Ac) | 140.02 | 177.62 | 7.3 | 26 | 1.18
Relation between Adsorption of Cu2+ with Surface Area, pH and Aromaticity
No evident relationschip between K, Kd and surface area or pH
Adsorption efficiency increases with aromaticity and decreasing polarity
Adsorption to charged groups as main mechanism is unlikely!!!
© Authors, all rights reserved

## Slide 13
Relaxation
Magnetic field
Thermal Equilibrium (starting point!)
Nuclear spins given into a static magnetic field will align themselves on two different energy levels according to the thermal equilibrium
A radio frequency-pulse (rf) moves spins from the lower to the higher energy level
Termination of the pulse allows the spins to return (relax) to their thermal equilibrium with the spin-lattice relaxation time rate, T1.
NMR Relaxometry for the Identification of Cu2+ Adsorption Sites:
Theoretical Background
© Authors, all rights reserved

## Slide 14
Short T1
Long T1
Molecular size / mobility:
Theoretical Background: T1 and Molecular Properties
Solid-state
Interaction with paramagnetics at a distance < 1 nm decreases efficiently T1
small
large
T1 depends on:
© Authors, all rights reserved

## Slide 15
Spin Diffusion: Spins in close neighborhood “communicate” their relaxation behavior among each other, which results in one common T1:
Theoretical Background: T1 and Domaine Size
The size of the „communication radius. L“
depends on T1:
Short T1
Long T1
Small
radius
Large radius
Kind of T1 | Time (ms) | L (nm)
T1roh-H | 0.1 – 20 | 2 - 30
T1H | 20-940 | 30 -160
T1C | 2000 -34000 | Non*
* The low natural abundance of 13C does not allow spin-diffusion
Kind and range of T1s used in the present study:
© Authors, all rights reserved

## Slide 16
Information Obtainable from the Determination of T1:
Identification of C groups which are affected by Cu2+ adsorption: T1C
Changes in molecular mobility: T1H, T1Hroh
Minimal distance between domaines: T1H, T1Hroh
Chemical composition of fast and slowly relaxing pool
Selecting an adsorption mechanism according to the results
© Authors, all rights reserved

## Slide 17
Chart: Carboxyl 185-160 ppm
| 0 | 4.8608099999999999 | 9.1338749999999997 | 12.517380000000001 | 18.267749999999999 | 19.061999999999998
T1Hrohs (us) | 1800 | 2760 | 2600 | 2542 | 2305 | 2650
Chart: 160-140 ppm
| 0 | 4.8608099999999999 | 9.1338749999999997 | 12.517380000000001 | 18.267749999999999 | 19.061999999999998
T1Hrohs (us) | 2910 | 2700 | 3200 | 3217 | 2910 | 3620
T1Hrohf (us) | 598 | 368 | 475 | 365 | 597 | 982
Chart: 140-130 ppm
| 0 | 4.8608099999999999 | 9.1338749999999997 | 12.517380000000001 | 18.267749999999999 | 19.061999999999998
T1Hrohs (us) | 2510 | 2990 | 3480 | 3217 | 2510 | 2650
T1Hrohf (us) | 598 | 368 | 475 | 365 | 597 | 982
Chart: 130-100 ppm
| 0 | 4.8608099999999999 | 9.1338749999999997 | 12.517380000000001 | 18.267749999999999 | 19.061999999999998
T1Hrohs (us) | 2750 | 3130 | 4440 | 3277 | 3340 | 3020
T1Hrohf (us) | 455 | 597 | 1150 | 408 | 686 | 609
Chart: O-Alkyl 90-45 ppm
| 0 | 4.8608099999999999 | 9.1338749999999997 | 12.517380000000001 | 18.267749999999999 | 19.061999999999998
T1Hrohs (us) | 2790 | 7770 | 3110 | 4558 | 2700
Chart: Alkyl 45-0 ppm
| 0 | 4.8608099999999999 | 9.1338749999999997 | 12.517380000000001 | 18.267749999999999 | 19.061999999999998
T1Hrohs (us) | 2750 | 3930 | 3170 | 3691 | 4070 | 2630
T1Hrohf (us) | 502 | 732 | 1490 | 349 | 1091 | 2170
0
1000
2000
3000
4000
0
1000
2000
3000
4000
0
1000
2000
3000
4000
slow
fast
0
5
10
15
20
0
5
10
15
20
127
125
123
OH
153
O
153
142
107
111
Furan-type
141
127
128
127
Biphenyl
COOH
165
T1Hroh versus Qe (Cu2+) in Ch400
© Authors, all rights reserved

## Slide 18
None or only weak but positive correlations between T1Hroh and Qe:
  Decrease of domain mobility after Cu2+ Adsorption overcomes shortening due to paramagentic interaction?
  Aromatic C and alkyl C show pools with fast and slow T1Hroh (no spin diffusion among them, thus no interactions)
  Domains with small and large molecules: Distance: > 7.5 nm
  Carboxyl C and O-alkyl C is only present in the slow fraction with higher molecular weight
  Located mostly in ether and ester bonds. This makes them unlikely to serve as cation-adsorption site
  T1Hroh is comparable for all peaks within one domain
  Efficient spin 1H spin diffusion does not allow the identification of a specific adsorption site
  Comparable results for Pe500
T1Hroh versus Qe (Cu2+) - conclusions
© Authors, all rights reserved

## Slide 19
T1Hroh Ac450 >> T1Hroh Ch400 = T1Hroh Pe500:
  Remaining crystalline cellulose-like units in Ac450
  Carboxyl, O-alkyl and alkyl show two domains
  Presence of amorphous units (short T1Hroh)
  T1Hroh short (carboxyl, alkyl) increases with Qe
  “Stabilization“ of amorphous domains?
  T1Hroh versus Qe of aromatic C shows no correlation
T1Hroh versus Qe (Cu2+) – Ac450
Chart: Carboxyl 185-160 ppm
| 0 | 0 | 3.9712499999999999 | 10.128276 | 6.3540000000000001 | 11.119499999999999
T1Hrohs (us) | 14940 | 13100 | 10403 | 12079 | 17329
T1Hrohf (us) | 225 | 413 | 283 | 641
Chart: O-Alkyl 90-45 ppm
| 0 | 0 | 3.9712499999999999 | 10.128276 | 6.3540000000000001 | 11.119499999999999
T1Hrohs (us) | 11700 | 14400 | 14418 | 13240 | 12939 | 12763
T1Hrohf (us) | 801 | 834 | 217 | 1011
Chart: Alkyl 45-0 ppm
| 0 | 0 | 3.9712499999999999 | 10.128276 | 6.3540000000000001 | 11.119499999999999
T1Hrohs (us) | 9900 | 11200 | 10974 | 10021 | 13569 | 9225
T1Hrohf (us) | 214 | 223 | 489
Chart: Aromatic C 130 -100 ppm
| 0 | 0 | 3.9712499999999999 | 10.128276 | 6.3540000000000001 | 11.119499999999999
T1Hrohs (us) | 11000 | 13200 | 14967 | 12083 | 12589 | 11228
T1Hrohf (us) | 1184 | 485 | 339 | 793
© Authors, all rights reserved

## Slide 20
For all C-groups the “one-pool”–fit works best
T1H O/N-alkyl (ether, N-alkyl; 90 – 45 ppm) > T1H aromatic C (160-100 ppm)
T1H of all C-groups are affected by Cu2+
Minimum T1H: aromatic C (20-30 ms) < O/N-alkyl C (50 – 60 ms)
→ aromatic C as the preferential adsorption site ?
T1H versus Qe (Cu2+) – Ch400, Pe500
Chart: T1H Pe500
| 4.6066499999999992 | 9.3721499999999995 | 19.856249999999999 | 19.061999999999998 | 0 | 4.6066499999999992 | 9.3721499999999995 | 15.287724000000001 | 19.856249999999999 | 19.061999999999998 | 0 | 4.6066499999999992 | 9.3721499999999995 | 15.287724000000001 | 19.856249999999999 | 19.061999999999998 | 0 | 4.6066499999999992 | 9.3721499999999995 | 15.287724000000001 | 19.856249999999999 | 19.061999999999998 | 0 | 4.6066499999999992 | 9.3721499999999995 | 15.287724000000001 | 19.856249999999999 | 19.061999999999998 | 0 | 4.6066499999999992 | 9.3721499999999995 | 15.287724000000001 | 19.856249999999999 | 19.061999999999998 | 0 | 4.6066499999999992 | 9.3721499999999995 | 15.287724000000001 | 19.856249999999999 | 19.061999999999998 | 0 | 4.6066499999999992 | 19.856249999999999 | 19.061999999999998 | 0 | 4.6066499999999992 | 15.287724000000001 | 19.856249999999999 | 19.061999999999998 | 0 | 4.6066499999999992 | 9.3721499999999995 | 15.287724000000001 | 19.856249999999999 | 19.061999999999998
185-160 ppm | 38 | 39 | 31 | 36
160-140 ppm | 60 | 26 | 28 | 20 | 25 | 26
140-130 ppm | 47 | 23 | 23 | 21 | 22 | 23
120-100 ppm | 51 | 22 | 20 | 22 | 21 | 20
90-60 ppm | 131 | 122 | 40 | 56
45-0 ppm | 88 | 44 | 32 | 26 | 38 | 37
60-45 ppm | 176 | 37 | 40 | 55 | 78
Chart: T1H Ch400
| 0 | 4.8608099999999999 | 9.1338749999999997 | 12.517380000000001 | 18.267749999999999 | 19.061999999999998
185-160 ppm | 197 | 61 | 26 | 35 | 42 | 29
160-140 ppm | 136 | 37 | 29 | 30 | 26 | 27
140-130 ppm | 126 | 38 | 29 | 28 | 23 | 24
120-100 ppm | 122 | 37 | 31 | 23 | 22 | 22
90-60 ppm | 356 | 91 | 32 | 69 | 56
45-0 ppm | 156 | 47 | 34 | 30 | 27 | 29
60-45 ppm | 342 | 175 | 54 | 57 | 54
© Authors, all rights reserved

## Slide 21
T1H versus Qe (Cu2+) – Ac450
Chart: Carboxyl C: 185-160 ppm
| 0 | 0 | 3.9712499999999999 | 10.128276 | 6.3540000000000001 | 11.119499999999999
slow | 978 | 555 | 887 | 669 | 633 | 610
Chart: Aromatic C: 120-100 ppm
| 0 | 0 | 3.9712499999999999 | 10.128276 | 6.3540000000000001 | 11.119499999999999
slow | 1130 | 663 | 992.684 | 881.06 | 872 | 842
fast | 1130 | 663 | 50.686 | 29.758 | 29.6 | 29
Chart: O-Alkyl C: 90-60 ppm
| 0 | 0 | 3.9712499999999999 | 10.128276 | 6.3540000000000001 | 11.119499999999999
slow | 1082 | 738 | 1041 | 605 | 934 | 814
fast | 1082 | 738 | 53.805 | 27.7 | 32 | 29
Chart: Akyl C: 90-60 ppm
| 0 | 0 | 3.9712499999999999 | 10.128276 | 6.3540000000000001 | 11.119499999999999
slow | 881 | 615 | 808 | 713.5 | 922 | 727
fast | 881 | 615 | 45.6 | 19.7 | 28.3 | 28.1
Without Cu2+, there is only one “pool”
Cu2+ (4 mg g-1) → 2 pools (T1H ≈ 50 ms → efficient spin diffusion < 35 nm)
T1H-slow stays almost constant
T1H-fast decreases with Qe
Minimum T1H for all C groups: 30 ms
Cu2+ adsorbs only on certain surfaces (pores are to small for entrance of Cu2+?)
1H spin diffusion affects only C in a radius < 35 nm
Core C (T1H-slow) with a distance > 35 nm
is not affected by Cu2+ adsorption
© Authors, all rights reserved

## Slide 22
T1C versus Qe (Cu2+) – ChCu400
Without Cu2+, there is only one “pool”
Cu2+ (4.8 mg g-1) → 2 pools
All aromatic C are affected by Cu2+
O-Alkyl C shows no evidence for adsorption
NO evidence for C with preferential sorption
Chart: 185-160 ppm
| 0 | 4.8608099999999999 | 9.1338749999999997 | 12.517380000000001 | 18.267749999999999 | 19.061999999999998
slow | 5.29 | 7.08 | 8 | 3.195 | 3.47
fast | 0.159 | 1.7 | 0.063
Chart: 160 - 140 ppm
| 0 | 4.8608099999999999 | 9.1338749999999997 | 12.517380000000001 | 18.267749999999999 | 19.061999999999998
slow | 26.4 | 5.95 | 4.14 | 6.7 | 3.024 | 4.57
fast | 26.4 | 0.301 | 0.179 | 0.7 | 0.284 | 0.83
Chart: 140 - 130 ppm
| 0 | 4.8608099999999999 | 9.1338749999999997 | 12.517380000000001 | 18.267749999999999 | 19.061999999999998
slow | 14.7 | 5.23 | 4.17 | 3.4 | 2.62 | 2.25
fast | 14.7 | 0.447 | 0.365 | 0.3 | 0.262 | 0.249
Chart: 130 - 100 ppm
| 0 | 4.8608099999999999 | 9.1338749999999997 | 12.517380000000001 | 18.267749999999999 | 19.061999999999998
slow | 11.6 | 5.75 | 5.06 | 3.9 | 2.494 | 2.89
fast | 11.6 | 0.452 | 0.556 | 0.5 | 0.224 | 0.511
Cation adsorption to π-orbitals of the aromatic rings?
© Authors, all rights reserved

## Slide 23
T1C versus Qe (Cu2+) – AcCu450
O-substituted groups show adsorption
No evidence for adsorption on alkyl C
Aromatic C shows 2 pools after Cu2+ addition
Cu2+ adsorption is different for Ac450 and ChCu400
Chart: Carboxyl C: 185-160 ppm
| 0 | 10.128276 | 6.3540000000000001 | 11.119499999999999
slow | 26.9 | 5 | 17.1 | 4.6
fast
Chart: Phenol C: 160 - 140 ppm
| 0 | 3.9712499999999999 | 6.3540000000000001 | 11.119499999999999
slow | 34.4 | 26.6 | 16.9 | 16.9
fast
Chart: O-Alkyl C: 90-60 ppm
| 0 | 0 | 3.9712499999999999 | 10.128276 | 6.3540000000000001 | 11.119499999999999
slow | 47.5 | 25.5 | 16.3 | 20.4 | 20.6 | 6.9
fast | 1.7 | 0.7 | 0.6 | 1 | 0.9 | 0.4
Chart: Alkyl C: 45-0 ppm
| 0 | 0 | 3.9712499999999999 | 10.128276 | 6.3540000000000001 | 11.119499999999999
slow | 33.6 | 17 | 7.6 | 9.6 | 36.9 | 23.5
fast | 1.4 | 0.4 | 0.2 | 0.9 | 1.1 | 0.2
Chart: C-aromatic C: 140 - 130 ppm
| 0 | 0 | 3.9712499999999999 | 10.128276 | 6.3540000000000001 | 11.119499999999999
slow | 32.1 | 33 | 25.4 | 19.6 | 23 | 11.8
fast | 32.1 | 33 | 25.4 | 0.8 | 0.9 | 0.4
Chart: Aromatic C: 130 -100 ppm
| 0 | 0 | 3.9712499999999999 | 10.128276 | 6.3540000000000001 | 11.119499999999999
slow | 23 | 23 | 16.8 | 22.2 | 37 | 8.7
fast | 23 | 23 | 1.1 | 1.4 | 0.3
© Authors, all rights reserved

## Slide 24
Conclusions
Cu2+ adsorption correlates best with aromaticity of the char, possibly because in the highly aromatic pyrochars, charged groups such as carboxyl or ether are involved in bridging the aromatic domains or within an crystalline domaine (Ac450) and thus not accessible for Cu2+.
Cu2+ did not or only slightly affect T1Hroh:
Effect of decreasing mobility due to chelating is more pronounced than the paramagnetic effects?
Smaller domain size (indicated by smaller T1H) of the highly aromatic chars offer more surface and thus more sites for adsorption than slightly charred material derived from woody residues (showing large T1H).
© Authors, all rights reserved

## Slide 25
Conclusions
In Ac450 containing both polar groups and aromatic structures, both groups are involved in the adsorption.
We have no evidence that alkyl C or methoxyl C were involved in the adsorption
Low Cu2+ adsorption in Ac450 may be best explained by crystalline structures, reducing the accessibility of Cu2+ to adsorption sites and the low content of aromatic C offering binding do their π-orbitals
© Authors, all rights reserved

## Slide 26
Thanks
To the organizers that made this online conference possible
MINECO (Spain) and FEDER (CGL2012-37041/CGL2015-64811-P)