## Slide 1: X-ray absorption analysis of Zn and Cu speciation in soils around the sediment ponds of chemical plants
Tatiana Minkina, Dina Nevidomskaya, Victoria Shuvaeva, Tatiana Bauer, and Marina Burachevskaya
Southern Federal University, Rostov-on-Don, Russia
tminkina@mail.ru

## Slide 2: D1
Object of study
The territory around the sediment ponds of chemical plants in the Severskii Donets floodplain in Rostov oblast, South of Russia
D4

## Slide 3
Physical and chemical properties Fluvisol (background soil D0) and Technosols (D4) of the investigated monitoring plots
Sample/Parameter | D0 (Control) | D4
Corg,% | 3.4±0.1 | 4.4±0.2
pHwater | 7. 3±0.2 | 7.7±0.3
СаСО3, % | 1.3±0.02 | 5.3±0.3
Exchangeable Ca2+, cmol(+)/kg | 31.0±2.4 | 35.2±1.7
Exchangeable Mg2+, cmol(+)/kg | 4.5±0.3 | 5.0±0.2
SO3, % | 0.8±0.02 | 7.3±0.1
Fe2O3,% | 7±0.2 | 6.0±0.1
Silt fractions (0.01-0.001 mm), % | 53.1±2.7 | 52.1±3.8
Clay fraction (<0.001 mm), % | 32.4±2.1 | 33.0±2.6
Pb (16*) | 20.1±1.7 | 1591.2±129.3
Cr (83) | 97.9±7.3 | 154.1±12.5
Ni (58) | 40.9±2.6 | 80.5±10.0
Mn (1000) | 230.4±66.9 | 426.1±51.0
Cu (47) | 43.7±3.2 | 146.9±10.4
Zn (83) | 90,0±7,6 | 66000±5903
Cd (0.13) | 0.2±0.003 | 10.6±1.0
(*) lithosphere clark (Vinogradov, 1957); excesses over the clarks are highlighted in bold

## Slide 4
Mineralogy composition Fluvisol (background soil D0) and Technosols (D4) of the investigated monitoring plots, %
*(tr) traces
**(nd) not detected
Sample | Terrigenic minerals |  |  |  |  |  |  |  |  | Autigenic minerals |  |  | 
 | Stable |  |  |  |  | Unstable |  |  |  |  |  |  | 
 | Rutil | Zircon | lmenite | Kyanit | Staurolite | Amphibole | Muscovite, biotite | Magnetite, hematite | Pyroxene | Iron hydroxides | Pyrite, marcasite | Carbonates | Sulfates
D0 (Control) | 4.0 | 8.0 | 5.0 | tr* | 4.0 | nd** | н/о | 57.0 | 3.0 | 13.0 | 1.0 | tr | 5.0
D4 | tr | tr | 12.0 | tr | nd | nd | nd | tr | nd | 20.0 | 8.0 | tr | 60.0

## Slide 5
Method of Sequential extraction
BCR three-stage sequential extraction scheme
Extraction stage and heavy metal fractions | Extracts
First: Water soluble, exchangeable and carbonate bound fraction | extraction with 0.11 mol/dm3 of acetic acid for 16 h at 22 ± 5 °C with constant stirring
Second: Reducible fraction (Iron/manganese oxyhydroxides) | extraction with 0.1 mol/dm3 Na2OH·HCl during 16 h with continuous stirring at pH = 2 (with the HNO3 input)
Third: Oxidizable fraction (Organic matter and sulfides) | 1) 2 h in water bath at temperature 85±2 ºC, dispersion H₂O₂ at pH = 2 2) 16 h in water bath at temperature 22 ± 2 oC, continuous stirring, dispersion 1.0 mol/dm³ NH₄OAc(CH₃COOHNH₄) at pH = 2 (with the HNO3 input)
Residual: residual fraction (soluble in oxidative acids) | includes dispersed metals with a mixture of concentrated hot acids HNO₃ and HCl

## Slide 6
Methods of study
The accumulation and speciation of Zn and Cu technogenically man-transformed soils within the anomaly zone were studied using a direct
nondestructive physical methods
X-ray Absorption Spectroscopy
(XANES and EXAFS)
X-ray Diffraction (XRD)
Scanning Electron Microscopy (SEM) and energy-dispersive X-ray (EDX) spectroscopy
Fragment of a large ring of the Kurchatov synchrotron
X-ray diffraction
SEM – CarlZeiss EVO-40

## Slide 7
Fraction composition of Zn and Cu compounds (mg/kg) in
Fluvisol (background soil D0) and Technosol (D4)
Zn
Cu
Monitoring plot | Fraction |  |  | 
 | acid-soluble | reducible | oxidisable | residual
Zn |  |  |  | 
D0 | 6.0±0.04 | 15.0±1.2 | 13.8±0.7 | 55.2±7.2
D4 | 1172 ±1069 | 29954±2356 | 2794±146 | 17559±1491
Cu |  |  |  | 
D0 | 0.6±0.1 | 1.6±0.1 | 4.4±0.6 | 37.1±2.8
D4 | 18.0±0.9 | 12.0 ±1.0 | 34.1±3.7 | 82.8±9.1
Background soil (D0)
Technosol (D4)
Background soil (D0)
Technosol (D4)
Fractionation of Zn in the Technosol unraveled a high degree of metal fixation with Fe–Mn (hydr)oxides and silicates. Cu is characterised by accumulation in the residual and oxidisable fractions.

## Slide 8
The XRD analysis unraveled the presence of authigenic S-containing minerals: sphalerite (cubic ZnS), würtzite (hexagonal ZnS), covellite (CuS) and bornite (Cu5FeS₄).
Synchrotron X-ray diffraction (XRD) of Technosol samples after the BCR selective sequential extraction

## Slide 9
After the removal of exchange Zn compounds from Technosol (First stage), the soil is enriched in a great diversity of metal compounds, primarily with Zn–S and Zn–O bonds. In the fraction associated with phyllosilicates, the Zn–О bond is the main component (50%). After extracting the first and second fractions, the Zn–S bond prevails as würtzite (hexagonal ZnS) that makes up more than 50%, in agreement with predominance of the Zn–O bond in the first shell based on the EXAFS data.
Diagnostics of Zn speciation in chemical fractions of the Technosol using synchrotron methods (XANES and EXAFS)
Zn K-edge XANES spectra of
fractions extracted
k2-weighted EXAFS oscillations in the Zn K-edge absorption spectra
9
Results of the modeling of experimental Zn K-edge XANES spectra of Technosol samples after different stages of the sequential fractionation and linear combinations of the spectra of reference compounds, % of the share of compounds in sample
Fractions | ZnSO4 | ZnO | ZnS
First stage (Exchangeable) | 65 | 0 | 35
Second stage (Reducible) | 0 | 50 | 50
Third stage (Oxidizable) | 25 | 18 | 57
Best fits of the Fourier transform
of Zn EXAFS spectra

## Slide 10
The results show that samples after the First stage are typically dominated by Cu2S and CuCO3. Spectra of soil samples after the Second stage match the Cu2S spectra with a high degree of accuracy, suggesting the prevalence of chalcocite in the given fraction. The soil sample after the third stage is characterised by a high content of CuCO3 (50% of all Cu compounds) and Cu2S (30% of all Cu compounds).
Diagnostics of Cu speciation in chemical fractions of the Technosols using synchrotron methods (XANES and EXAFS)
10
Results of the modeling of experimental Cu K-edge XANES spectra of Technosol samples after different stages of the sequential fractionation with the linear combination of reference compound spectra, % of the share of compounds in sample
Fractions | CuSO4 | CuCO3 | Cu2S | CuS | CuCl2
First stage (Exchangeable) | 4 | 0 | 86 | 0 | 10
Second stage (Reducible) | 0 | 0 | 100 | 0 | 0
Third stage (Oxidizable) | 12 | 50 | 33 | 0 | 0
Cu K-edge XANES spectra of
fractions extracted
k2-weighted EXAFS oscillations in the Cu K-edge absorption spectra
Best fits of the Fourier transform
of Cu EXAFS spectra

## Slide 11
SEM images of the newly formed minerals of Zn and Cu along with EDX spectra
Zinc speciation occurs as ‘crusts’, aggregates with calcite and gypsum
The EDX spectra revealed that metal concentrations are higher than the detection limit of ~0.05 wt %. The main concentrator of Zn phase is represented by the aqueous sulphate, goslarite (ZnSO4•7H2O) produced after the oxidation of zinc sulphate, and würtzite (ZnS). It has been established that Zn can make up both eigenphases and bonds with clay minerals or carbonates. The latters tend to adsorb actively Zn and fix it on the surface. High Cu concentration (> 0.05 wt %) was recorded only in the bond with clay aggregates.
The EDX spectra of Technonol's microaggregats. wt %
О | Al | Si | S | Ca | Fe | Zn
14.3 | 0.5 | 0.8 | 23.1 | 3.3 | 1.7 | 43.3

## Slide 12
CONCLUSION
Zn and Cu speciation in the highly contaminated Technosol was studied based on the XAFS, XRD and SEM methods after each stage of the sequential extraction procedure.
• Phyllosilicates and Fe-Mn (hydr)oxides are the main stabilizers of Zn mobility. Cu is characterised by accumulation in the residual and oxidisable fractions.
• The number of compounds with a higher solubility decreases at the subsequent stages of extraction.
•After first stage, the residual soil is enriched of with Me–S and Me–O bonds. In the residual soil left after extracting first and second fractions, the Zn–S bond prevails as würtzite (ZnS), while the Cu–S bond is represented only by chalcocite (Cu2S).
.

## Slide 13: Thanks The reported study was funded by Russian Foundation for Basic Research, projects no. 19-34-60041 and 19-05-50097