## Slide 1
Thallium mobility in mining wastes at the Crven Dol locality, Allchar deposit,
North Macedonia
Tamara Đorđević
Institut für Mineralogie und Kristallographie, Universität Wien, Wien, Austria
tamara.djordjevic@univie.ac.at
Uwe Kolitsch
Mineralogisch-Petrographische Abteilung, Naturhistorisches Museum, Wien, Austria
Petr Drahota, Magdaléna Peřestá
Institute of Geochemistry, Mineralogy and Mineral Resources, Faculty of Science, Charles University, Czech Republic
Juraj Majzlan, Stefan Kiefer
Institute of Geosciences, Department of Mineralogy, Friedrich-Schiller-Universität, Jena, Germany
Tomáš Mikuš
Earth Science Institute, Slovak Academy of Sciences, Geological Division, Banská Bystrica, Slovakia
Todor Serafimovski, Goran Tasev, Blažo Boev
Department of Mineral Deposits, Faculty of Natural and Technical Sciences, University “Goce Delčev”-Štip, Macedonia

## Slide 2
2
Objectives
Characterization of the crystalline primary and secondary Tl-minerals
Characterization of amorphous and poorly crystalline secondary Tl-minerals
Quantify the distribution of thallium and evaluete geochemical controls on dissolved Tl and As

## Slide 3
3
Allchar
deposit
Allcahr deposit: position

## Slide 4
4
from 1881 to 1913: excavation of arsenic ore
from 1953 to 1965 and from 1970-1973: excavation of
low-grade antimony ore
late 1980s: discovery of thallium minerals (lorandite, vrbaite etc.) as constituents of the arsenic-antimony ore
special interest for thallium from lorandite as a possible solar neutrino detector  systematic investigations of thallium mineralization in the northern part of the Allchar deposit (Crven Dol ore body)
geological, geochemical, mineralogical and hydrothermal alteration features are similar to Carlin-type mineralization of the Western United States.
Allcahr deposit: generalities

## Slide 5
5
Allchar and Crven Dol: Geology
Geological map of the Allchar ore deposit after Boev et al. (2016)
Boev, B. et al. (2016): Geologica Macedonica, 30, 115-127; Amthauer et al. (2016): Miner. Petrol., 105, 157-169.
Crven Dol
(edit 21)
Geological profile of Crven Dol after Amthauer et al. (2012)

## Slide 6
6
Hydrothermal alteration
  Modereate to strong agrilic alteration is widesprad
  Dolomitization
  Weak, localized silification
Crven Dol (edit 21): site description
Types of mineralization
  Abundant thallium mineralization (mostly Tl-sulfosalts)
  Abundant arsenic mineralization (realgar, orpiment, sulfosalts)
  Oxidation zone scarcely investigated
Geochemical characteristic
  As + Tl >> Sb + Hg + SiO2
  As:Sb, Tl:Sb  increasing
  SiO2, Au+Sb  decreasing

## Slide 7
7
Sampling
Waste dumps at Crven Dol: 41°1595N, 21°9514E
CD-18-2
CD-18-4
CD-18-1
CD-18-3
CD-18-3

## Slide 8
8
Sampling
Pore-water sampling at the waste dumps of Crven Dol:
41°1595N, 21°9514E
CD-18-1A,B,C
CD-18-2A,B,C
CD-18-2A,B,C
CD-18-3A,B,C

## Slide 9
9
Chemistry: ICP-OES and ICP-MS
Chart: Crven Dol chemistry (< 2mm)
| CD-18-1 | CD-18-2 | CD-18-3 | CD-18-4
Mn [mg kg-1] | 3734.3403 | 3078.7235 | 3136.5785 | 1430.4042
Fe [mg kg-1] | 47076.1488 | 26959.7132 | 232856.4805 | 9504.0341
As [mg kg-1] | 10505.0732 | 14269.1112 | 142057.7667 | 10028.67
Tl [mg kg-1] | 1065.7797 | 744.6931 | 14184.2746 | 717.1765
Chart: Crven Dol chemistry (< 0.063 mm)
| CD-18-1 | CD-18-2 | CD-18-3 | CD-18-4
Mn [mg kg-1] | 1712.5855 | 2708.9704 | 3333.1072 | 2505.3933
Fe [mg kg-1] | 6145.4117 | 16553.9695 | 182150.2058 | 34350.2627
As [mg kg-1] | 6985.9159 | 11333.8783 | 117315.8081 | 9471.0955
Tl [mg kg-1] | 725.7449 | 562.8367 | 17576.9857 | 901.6618

## Slide 10
10
Mineralogy of Crven Dol
Mineral name | Formula
Sulfates | 
Barite1,2 | BaSO4
Gypsum1–3 | CaSO4·2H2O
Dorallcharite1–3 | Tl0.8K0.2Fe3(SO4)2(OH)6
Jarosite1,2 | KFe3+3(SO4)2(OH)6
Hydroniumjarosite1–3 | (H3O)Fe3+3(SO4)2(OH)6
Phosphates | 
Fluorapatite1,2 | Ca5(PO4)3F
Xenotime-(Y)1 | Y(PO4)
Arsenates | 
Scorodite1–3 | Fe3+AsO4·2H2O
Pharmacosiderite1,2 | KFe3+4(AsO4)3(OH)4·6-7H2O
Natropharmacosid.1,2 | (Na,K)Fe3+4(AsO4)3(OH)4·6-7H2O
Thallium arsenate1–4 | new Tl mineral
Talmessite1–3 | Ca2Mg(AsO4)2 · 2H2O
Wallkilldellite1,2 | Ca2Mn2+3(AsO4)2(OH)4·9H2O
Arseniosiderite1,2 | Ca2Fe3+3(AsO4)3O2·3H2O
Silicates | 
Muscovite1,3 | KAl2(AlSi3O10)(OH)2
Flogopite1 | KMg3(AlSi3O10)(OH)2
K-feldspar1 | K(AlSi3O8)
Albite1 (Ca-rich) | Na(AlSi3O8)
Kaolinite1 | Al2(Si2O5)(OH)4
Spessartine3 | Mn2+3Al2(SiO4)3
Mineral name | Formula
Sulfides and sulfosalts | 
Pyrite1–4 | FeS2
Marcasite3,4 | FeS2
Pyrrhotite3 | Fe1-xS
Realgar1–5 | As4S4
Oripiment1–5 | As2S3
Raguinite1,2 | TlFeS2
Picotpaulite1,2 | TlFe2S3
Cinnabar1 | HgS
Lorandite1–5 | TlAsS2
Fangite1,2 | Tl3AsS4
Jankovićite | Tl5Sb9(As,Sb)4S22
Oxides | 
Quartz1-4 | SiO2
Magnetite1 | Fe2+Fe3+2O4
Ulvöspinel1 | Fe2+2Ti4+O4
Ilmenite | Fe2+TiO3
Goethite3 | FeO(OH)
Fe-oxyhydrohides1,2 | 
Mn-oxides1,2,3 | 
Anatanse3 | TiO2
Carbonates | 
Calcite1–4 | CaCO3
Dolomite1–4 | CaMg(CO3)2
Siderite1 | FeCO3
1SEM-EDS, 2EPMA, 3Raman, 4PXRD, 5SXRD
Newly identified within this study
Italic: type locality

## Slide 11
Mineralogy: primary thallium minerals
Thallium sulfosalts: SEM and microprobe
Lorandite (TlAsS2) intergrown with realgar and scorodite
Raguiniter (TlFeS2) embedded in realgar
Picotpaulite (TlFe2S3) and As-bearing pyrite in realgar
100 m
fng
orp
lor
rel
sco
Fangite (Tl3AsS4) filling the cracks in orpiment
rel
rag
10 m
10 m
rel
ppaul
Py
100 m
lim
11

## Slide 12
12
Two generations of thallium arsenate (lighter and darker) intergrown with dolomite and arseniosiderite.
Mineralogy: thallium sources
New thallium arsenate: SEM and microprobe
10 m
100 m
dol
asid
asid
Tl-arsenate
10 m
Zone builing of thallium arsenates intergrown with arseniosiderite.
asid
Tl-arsenate
100 m

## Slide 13
Dorallcharite and hydroniumjarosite: SEM and microprobe
Fine-grained aggregates of dorallcahrite intergrown with Fe-oxo-hydroxides.
Dorallcharite, Tl0.8K0.2Fe3(SO4)2(OH)6 platelets
Tiny crystals of Tl-bearing hydroniumjarosite, (H3O,Tl)Fe3+3(SO4)2(OH)6
Mineralogy: secondary thallium minerals
10 m
10 m
doral
doral
FOH
lor
rel
10 m
sco
hjar
10 m
Spherulitic aggreagtes of dorallcahrite in realgar.
doral
rel
dol
13

## Slide 14
Raman spectra of thallium secondary minerals
Dorallcharite-hydroniumjarosite,
Tl0.8K0.2Fe3(SO4)2(OH)6-(H3O)Fe3(SO4)2(OH)6
Thallium arsenate:
unknown mineral species
Mineralogy: secondary thallium minerals
14

## Slide 15
Geochemistry: pore water
Chart: 
| CD_18_1A | CD_18_1B | CD_18_1C | CD_18_2A | CD_18_2B | CD_18_2C | CD_18_3A | CD_18_3B | CD_18_3C | CD_18_4A
As | 137.8 | 88.3 | 82.29 | 195.5 | 159.5 | 149.8 | 17.22 | 1.002 | 4.795 | 9.042
Chart: 
| CD_18_1A | CD_18_1B | CD_18_1C | CD_18_2A | CD_18_2B | CD_18_2C | CD_18_3A | CD_18_3B | CD_18_3C | CD_18_4A
Tl | 89.77 | 102.7 | 77.29 | 660 | 114 | 356 | 76.77 | 611.8 | 53.93 | 58.82
15

## Slide 16
16
Geochemistry: extractions

## Slide 17
Geochemistry: extractions
17

## Slide 18
Takeaways
pore water contained high aqueous concentrations
of thallium and arsenic
weathering of primary Tl-minerals in the near-surface oxidizing, partly acidic and temporarily wet environment releases significant amounts of As and Tl which are hosted differently in the secondary minerals
mild extractions mobilized up to 44% of the total Tl and 23% of the total As, indicating that a large amount of these toxic elements is bound weakly to solids and can be easily mobilized into the pore water
thallium occured in several secondary forms (dorallcahrite, new thallium arsenate, Tl-bearing hydroniumjarosite and Tl-bearing pharmacosiderite) and is also associated with Mn-oxides
18

## Slide 19
19
Thank you for your interest!
Feel free to contact me for your comments and questions.
Financial support of the Austrian Science Fund (FWF) [P 30900-N28] is gratefully acknowledged

## Slide 20
Tamara Đorđević is senior postdoctoral researcher and lecturer at the Institute of Mineralogy and Crystallography, University of Vienna. Her scientific interest focuses on: implementation of hydrothermal and ionothermal techniques for the synthesis of different classes of hydroxyl oxo- salts and hydrated oxo-salts; on the transformation of sulfidic mine wastes under environmentally relevant conditions; and on the development of structure-based hierarchies of various synthetic mineral-like oxo-salts in relationship to their environmental stability. She mostly teaches and mentors students in subjects associated with mineral synthesis and environmental mineralogy.
Her research topics encompass work implementing synthesis and crystallization techniques (hydrothermal/ionothermal crystal growth, solid-state synthesis), characterization of static and dynamic structures (electron microscopy including TEM and SEM, sXRD and pXRD, micro-Raman and IR spectroscopy) and geoscientific fieldwork. She was involved in fifteen scientific projects, in eleven of which she was a project leader.
Contact: tamara.djordjevic@univie.ac.at
About the presenting author:
www.univie.ac.at/Mineralogie/djordjevic.htm
20