## Slide 1: A Feasibility Investigation for Developing Artificial Beachrocks: A Potential Measure for Coastal Protection in Southeast Yogyakarta Coast, Indonesia
Lutfian R. Daryono1*, Kazunori Nakashima2, Satoru Kawasaki2, Koichi Suzuki3, Anastasia D. Titisari4, Didit H. Barianto4, Imam Suyanto5, and Arief Rahmadi5
1Laboratory of Biotechnology for Resource Engineering, Division of Sustainable Resources Engineering, Grad. School of Engineering, Hokkaido University, Japan
2Laboratory of Biotechnology for Resource Engineering, Division of Sustainable Resources Engineering, Faculty of Engineering, Hokkaido University, Japan
3Laboratory of Global Resources and Environmental System, Division of Sustainable Resources Engineering, Faculty of Engineering, Hokkaido University, Japan
4Department of Geological Engineering, Faculty of Engineering, Universitas Gadjah Mada, Yogyakarta, Indonesia
5Sub-department of Geophysics, Faculty of Mathematics and Sciences, Universitas Gadjah Mada, Yogyakarta, Indonesia

## Slide 2: Introduction
Coastal erosion is a natural process which poses serious problems to coastal communities worldwide.
Conventional engineering solutions have succeeded in combatting the erosion problem over decades.
However, they are associated with numerous problems as mentioned below.
Hard engineering solutions
Expensive, short lived, not environmentally friendly, large visual impact, interfere local wave hydrodynamics
Need periodic maintenance
In need of more ecofriendly, inexpensive novel approaches
Breakwater
Seawall
Revetment
Sea groyne
Artificial corals
Sand dunes
Green belts
Nourishment
Soft engineering solutions
Lab. Biotechnology for Resources
Notes: Continual and costly maintenance work
Large visual impact
Downdrift erosion in the presence of alongshore currents

## Slide 3: Natural beachrock as a model: A Lesson learnt from nature
Beachrocks are sedimentary formations resulted from lithification of beach sediments by carbonate cementation
They have been identified as a natural barrier against coastal erosion
Buried
Outcrops
Submerged
Natural beachrock
Region of concern
Buried
Outcrops
Artificial beachrocks
?
Introduction
Lab. Biotechnology for Resources
Notes: At the same time

## Slide 4
Construction Biotechnology
Biotechnology for Construction Materials
Biotechnology for Construction Processes
Construction Bioplastics
Microbial additions to cement, mortars, and grouts
Microbial cements, mortars, and grouts
Biocementation
Bioclogging
Bioremediation
Biodesaturation
Bioaggregation
Biocrusting
Biocoating
Biotechnology is a scientiﬁc and engineering knowledge on the use of microorganisms or their products in large-scale industrial processes.
Biotechnology background

## Slide 5: Microbiologically-influenced
Biocorrosion and biodeterioration caused by microbial activity
For example, pigeon poo blamed for bridge collapse at Minnesota bridge (2007) which killed 13 people.
Nitric Acid

## Slide 6
Urea is hydrolysed by microbial urease which causes calcium carbonate to precipitate in the presence of a calcium source.
Overall cementation
Bacterial cells acting as nucleation sites
Microbial Induced Carbonate Precipitation
Loose sand grains are then bound together by the resulting calcium carbonate biocement.
Laboratory of Biotechnology for Resources

## Slide 7
Assessing the feasibility of natural beachrock sedimentation to develop bioaugmentation as an eco friendly alternative against coastal erosion.
Aim
Objectives
Understand the coastal evolved sedimentary carbonate toward beachrock phenomena and examine the relations among the operation parameters
Address mechanical behavior and microstructure of the natural beachrock for based information to develop artificial rocks
AIMS AND OBJECTIVES
Lab. Biotechnology for Resources

## Slide 8
Original inoculum
5g beachrock/ beach sand 45 ml of distilled water
10-1
10-2
10-3
10-4
10-5
1 ml
1 ml
1 ml
1 ml
1 ml
Serial dilutions (9 ml of distilled water in each case)
Plating
24 hrs
24 hrs
24 hrs
45C
Separation
Screening
Isolation
Urease activity test
DNA extraction and identification of bacteria
Culture medium
Land bacteria – NH4-YE
Sea bacteria – Zobell 2216E
50 μl from each dilution
METHODOLOGY
Isolation and Identification of ureolytic bacteria

## Slide 9
Bacteria in solid culture medium
5 ml of
pre-culture
24 hrs,
160 rpm
100 ml of main culture
1 ml for urease activity test by Indopheneol method
Cell growth in terms of OD at 600 nm
ZoBell2216E medium (5.0 /L hipolypeptone , 1.0 g/L FePO4 and 1.0 g/L yeast extract)
The intensity of the blue color which is proportional to [NH4+] is measured using UV-Vis spectrophotometer. The rate of urea hydrolysis is calculated using a calibration curve.
METHODOLOGY
Determining bacterial cell growth and urease activity
Composition of culture medium
Urease activity test by Indophenol method
1 ml of bacteria culture is added to 0.1 M urea solution in 0.1 M sodium phosphate buffer. The resulting NH4+ ions react with added phenol in the presence of hypochlorite and forms a blue colored indophenol.

## Slide 10: STUDY AREA
α-location
Krakal-Sadranan Beachrock UAV Drone Mapping
Most prone to erosion of sandy slopes due to strong waves created by South Western monsoon
Lab. Biotechnology for Resources

## Slide 11: RESULTS AND DISCUSSION I
Lab. Biotechnology for Resources
Beachrock
Carbonate Sands
Three important Major Oxide Element formed Beachrock Solidification, whereas CaO, MgO, and Na2O

## Slide 12
Results and discussion I
Laboratory of Biotechnology for Resources
Evaluation of the efficiency MICP using local strain bacteria
Pseudoalteromonas tetradonis sp.
Oceanobacillus profundus sp.
Vibrio maritimus sp.

## Slide 13
SMALL SCALE SAND SOLIDIFICATION TEST
Two phase injection: cycles of batch treatment of bacteria suspension and cementation solution
Bacteria suspension
OD600 = 2.0-2.5
Bacteria Fixation
Phase 1
Cementation solution
Phase 2
Saturated
condition
35 ml or 50 ml syringes
Filter papers
Sand compacted in the column
Silicon tube outlet
1.0 M Ca2+ cementation solution (g/l) | 
CaCl2 | 55.49
Urea | 30.03
Nutrient broth | 3.0

## Slide 14
Results and discussion II
Laboratory of Biotechnology for Resources
Evaluation of the efficiency MICP using local strain bacteria
Pseudoalteromonas tetradonis sp.
Oceanobacillus profundus sp.
Vibrio maritimus sp.
Mix bacteria between
psedoalteromonas and oceanobacillus
Psedoalteromonas sp.
Oceanobacillus sp.
Control
Pathogenic
Weak solidification
Fine Silica Sand
Coarse Sand
Biosafety level 1
Biosafety level 1
Biosafety level 1

## Slide 15
Effect of Grain Size Distribution on Sand Solidification by MICP
(a)
(b)
(c)
Toyoura
(D50 =
0.2 mm)
Mikawa
(D50 = 0.87 mm)
Coarse Beach sand
(D50 =
0.57 mm)
Height of the column (cm)
Silica Beach sand
(D50 =
0.3 mm)
0
4
6
8

## Slide 16
Rhombohedral calcite crystals were dominant in all cases
CaCO3 bond
Cladding on sand grains
Glass Beads grain
MORPHOLOGY OF THE CaCO3 CRYSTALS
Glass Beads grain

## Slide 17
PROPOSED METHODOLOGY based on MICP
End of slides
Conceptual Design
Vertically exaggerated
Region of concern
Surface zone sand stabilized by MICP
MLT
MHT
GWL
Should follow the topology of natural beachrocks
Should have sufficient strength
Should be permeable enough to allow seawater flow
Should be economically feasible
Should be environmentally friendly
Should resist abrasion and scouring
Requirement for treatment of hazardous ammonium by-products
Long term durability of the structure under wave action
Limited applications for fine grained soils
Implications for the Target Application
In-situ stabilization of loose beach sand with minimum disturbance to the local hydrodynamics
Self-recovering capability of the biocemented layer by dissolution and re-precipitation of carbonate minerals
Environmentally friendly
Low energy consumption
Relatively cheaper in long run
Insight into the Benefits of MICP