## Slide 1
Dislocation nucleation at nanoscale fluid inclusions:
Direct observation from atom probe tomography data
of naturally deformed pyrite
Renelle Dubosq (Ottawa)
Anna Rogowitz (Vienna)
Kevin Schweinar (Düsseldorf)
Baptiste Gault (Düsseldorf)
David A. Schneider (Ottawa)
pinning

## Slide 2
strain hardening
strain softening
Mineral rheology
A mineral’s response to stress is dependent on dislocation activity
obstruction of dislocation movement by dislocation entanglement or pinning
steady-state
localization of deformation in shear zones of brittle slip planes
continued generation and migration of dislocations
*segregation of trace element in dislocations can obstruct its movement

## Slide 3
Approach
2D microstructural analysis
2D & 3D nanostructural and chemical analysis
-Electron backscatter diffraction (EBSD)
-Electron channeling contrast imaging (ECCI)
-Atom probe tomography (APT)
-Scanning transmission electron microscopy (STEM)
We have combined 2D and 3D micro- and nano-analytical techniques on naturally deformed pyrite to investigate the interaction between crystal-defects and trace elements during deformation and its impact on mineral rheology.
(https://ccem.mcmaster.ca/atom-probe-tomography/)
(https://www.mpie.de/3079126/ECCI)

## Slide 4
2D microstructures
EBSD misorientation and grain boundary map
ECC image
low-angle grain boundary
• heterogeneous misorientation pattern
• maximum misorientation ~8
• ‘apparent’ low-angle grain boundary development at higher strain domains
• high-dislocation density
• low-angle grain boundary development
at tip of microfractures
dislocation
low angle
grain boundary

## Slide 5
Distance (nm)
Composition [As; O; at%]
Composition [Na; K; at%]
250 nm
As
O
Fe
3D nanostructures: specimen 1
APT reconstruction
2D contour plot of structure 1
structure 1
X
X’
X
X’
As
O
Na
K
dislocation
fluid inclusion

## Slide 6
3D nanostructures: specimen 2
1.0
0.0
at% [As]
50 nm
240 nm
As
O
Fe
APT reconstruction
2D contour plot of structure 1
structure 1
dislocation
fluid inclusion
Fluid inclusions are defined by apparent As-rich clusters topped by O-rich discs (confirmed with numerical modeling in Dubosq et al. 2020, Ultramicroscopy)
Dislocations are defined by As-rich linear structures
Dislocations are linked to 1 or 2 fluid inclusion(s)

## Slide 7
STEM images
2D nanostructures
fluid inclusion
Fluid inclusions are defined by dark spherical features
Dislocations are defined by discrete curved (”bowed”) line segments
Dislocations are linked to 1 or 2 fluid inclusion(s)

## Slide 8
Dislocation dilemma
Are dislocations nucleating in the local stress field of fluid inclusions (Fi) or are they being pinned by them?
dislocation nucleation
dislocation pinning
Fi
dislocation
dislocation
(modified from Vitik et al. 2000)
(modified from Vitik et al. 2000)
Dislocations nucleated at fluid inclusions and migrating away by dislocation glide
Dislocations pinned at fluid inclusions and middle segments migrating away by dislocation glide forming bowed configuration
Based on previous observations, we propose that the dislocations in our sample are being pinned by fluid inclusions rather than being nucleated at their local stress field since we only observe single dislocations linked to fluid inclusion with a bowed configuration and none that have migrated away from the inclusions.

## Slide 9
Summary
The investigated sample was deformed in the brittle to brittle-plastic regime
Our data reveal ubiquitous fluid inclusions defined by As-, O-, Na-, and K-rich element clusters
Dislocations are enriched in As and are linked to fluid inclusions
Dislocations were pinned at the stress field of fluid inclusions, which initiated the pipe diffusion of As from the fluid inclusions into the dislocation cores
Dislocations pinned at fluid inclusions could be potential source for Frank-Read dislocation generation sites

## Slide 10
Implications for mineral rheology
The way a mineral responds to an applied stress depends on two competing processes:
1) continued generation and migration of dislocations
vs
2) pinning and entanglement of dislocations
plastic regime
brittle regime
In our sample, dislocation pinning at fluid inclusions, which was further enhanced by trace element segregation in dislocation cores through pipe diffusion, resulted in a brittle dominated deformation regime confirmed by EBSD and ECCI data.
Nanostructural analysis can help predict a material’s physical properties and rheology